## Slide 1: Direct calculation of neutron diffraction on nanodiamonds
Shapiro Dmitrii
Institute of nuclear physics, Almaty, kazakhstan
UCN and VCN Source at the Institute of Nuclear Physics, Kazakhstan and their applications, 09.04.24

## Slide 2: Outline
  Nanodiamond application
  Why calculate diffraction on nanoparticles
  Cross-section calculation
  Program verification
  Orientation average

## Slide 3: Nanodiamonds application
  Diamond nanoparticles are promising reflectors of slow neutrons
    High albedo for VCN
    High quasispecular reflectivity for CN
  Such reflectors may be used to design a new generation of VCN/UCN sources, significantly increasing their intensity
  May be used at a new VCN/UCN source currently designed at WWR-K reactor of Institute of Nuclear Physics in Almaty, Kazakhstan
  More details in today’s report of Alexander Nezvanov at 14:00 “Nanodiamond reflectors for an intense source of very cold neutrons: properties and applications”

## Slide 4: Neutron propagation in nanodiamond powders
  Design of nanodiamond reflectors  calculation of neutron transport
  Existing model of VCN and CN propagation (report of Alexander Nezvanov )
    Based on experimental SANS data
    Not suitable for (Bragg diffraction)  diffraction calculation
  Existing NCrystal library for neutron scattering
    No influence of crystallite size on the Bragg peaks broadening
  Improved model (Wolfram Mathematica):
    Diffraction contribution to the scattering cross-section
    Nanodiamond size contribution to the Bragg peaks broadening
    Application for small neutron wavelengths

## Slide 5: Cross-section calculation
  Direct sum of scattered waves produced by diamond atoms in a nanoparticle
  Plane wave of incident neutron beam:
  Plane wave from 0 atom at :
  Plane wave from atom at :
Incident beam
Scattered beam
To the detector at 

## Slide 6: Cross-section calculation
  Plane wave from allatoms at :
  Differential cross-section:
  Total cross-section:
n
n
n
n

## Slide 7: Program verification: SANS
  Large object ()  small scattering angle
  Diamond nanoparticle , thermal neutrons
  Momentum transfer:
  SANS amplitude:
  SANS differential cross-section:

## Slide 8: SANS: -dependence
  Spherical nanoparticle with
  Neutron wavelengths

## Slide 9: SANS: -dependence
  Spherical nanoparticle with
  Scattering angles

## Slide 10: SANS: -dependence
  Spherical nanoparticles with
  Scattering angle
  Neutron wavelengths

## Slide 11: Program verification: large wavelength
  Total cross-section with :

## Slide 12: Program verification: Laue function
  Scattering amplitude of rectangular parallelepiped crystal:
  Structure factor:
  Laue function:
  Differential cross-section:
  Number of unit cells in a crystal:

## Slide 13: Program verification: Laue function
  Cubic nanoparticle with ()
  Diffraction on (111):

## Slide 14: Program verification: peak amplitudes
  SANS close to 0:
  Diffraction close to Bragg angle:

## Slide 15: Program verification: peak amplitudes
  For a diamond:

## Slide 16: Work in progress: orientation average
  Comparison with the experimental data (ILL, Grenoble)  orientation average
  Orientation  reciprocal lattice vector direction
  Random orientation  uniform distribution over solid angle:

## Slide 17: Conclusions
  Accounting for diffraction and finite nanoparticle size is essential for modeling of neutron transport in nanopowders
  The developed program allows to calculate scattering cross-section on the stationary nanoparticle
  So far the program has passed all the verification tests
  The next necessary step is nanoparticle orientation average

## Slide 18: Thank you for attention!